| PHYSICAL SPECIFICATION |
| --- |
| Nominal Voltage Nominal Capacity (20HR) | 12V 9Ah |  |
| Dimension | Length Width Container Height Total Height | 151±1mm （5.94 inches) 65±1mm (2.56 inches) 111±1mm (4.37 inches) 118±1mm (4.65 inches) |  |
| Weight | Approx. 3.15 Kg (6.94lbs) |  |
| Standard Terminal | Fasten Tab No.187E |  |
| ELECTRICAL SPECIFICATION |
| Characteristics | Discharge curves @ 25℃ (77 °F) |
| Capacity | 20 hour rate (0.45A) 10 hour rate (0.81A) 5 hour rate (1.53A) 3 hour rate (2.25A) 1hour rate (5.4A) | 9Ah 8.5Ah 7.7Ah 6.8Ah 5.4Ah |  |
| Capacity affected by temperature | 40℃ （104 0F） 25℃ （77 0F） 0℃ （32 0F） | 102% 100% 85% |  |
| Internal Resistance | Full charged battery (25℃,77 0F) 25mΩ |  |
| Constant Voltage Charge | Cycle | Initial Charging Current less than 2.7A Voltage 14.4~15.0V at 25℃ (77 0F ) Temperature Coefficient –30mV/℃ |  |
|  | Standby | No limit on Initial Charging Current Voltage 13.5~13.8V at 25℃ (77 0F ) Temperature Coefficient –20mV/℃ |  |